## Slide 1: clay mineralogical studies for greek bronze age Roofing technology
Christine M. Shriner, Erika R. Elswick, Hannah L. Timm, and Haydn H. Murray
Dept. of Geological Sciences, Indiana Univ., Bloomington, IN, USA

## Slide 2
MAP OF THE AEGEAN COMPLEX AT 2400 B.C.
1 - Lerna
2 - Kolonna
3 - Tiryns
4 - Thebes
5 - Zygouries
6 - Akovitika
Corridor House Examples

## Slide 3
Lerna, area plan. (After Caskey 1958; Wiencke, 2000)

## Slide 4
Lerna, final view of the House of Tiles. (Wiencke, 2000)

## Slide 5
Tiles, House of Tiles

## Slide 6
HT-2
Tile FTP

## Slide 8
Number 20 Phyllite
Number 19 Phyllite
CHS Chloritoid
Mercouri sample

## Slide 9
HT-3
HT-7
HT-14
HT-18
Eaves, House of Tiles

## Slide 10: XRD ANALYSIS
► X-ray diffraction analysis was undertaken on the eaves, as well as samples from the local schist (metaflysch), Pindos and Tripolis flysch deposits.
► The clay mineralogy is chlorite, illite and kaolinite, with accompanying quartz, calcite and feldspar.
►The lack of calcite in the potential source phyllites and schists was a tip off. The HT eaves have a 15-20% calcite component.

## Slide 11
► It does not become a question of “looks more like” a flysch than a metaflysch.
► It becomes a question of whether the eaves indicate “something else”.
► THE ARTIFACTS BECOME A RAW MATERIAL REFERENCE!

## Slide 12
GEOLOGICAL PERSPECTIVE

## Slide 13
After: Philpots and Wilson (1994)

## Slide 15
After: Saccani and Photiades (2005)

## Slide 16
The Phyllite Problem
15: Post-Maistichtian flysch of Pindos Zone
13: Radiolarites, pelites with pelagic limestones and the “first flysch”
10: Tripolis flysch, with Paleochora formation on top
8: Lower-middle Trias of Tyros Beds (with limestones, shales and tuffs)
7: Upper Paleozoic of Tyros Beds (with limestones, shales, tuffs and vulcanites)
6: Metaflysch
5: Transitional beds to the metaflysch
After Lekkas and Papanidolaou, 1977

## Slide 17: GEOLOGICAL AND ARCHAEOLOGICAL IMPLICATIONS
► HT eaves are not a schist or phyllite. Define HT eaves as an “argillite”.
► The very nature of argillite as a very indurated, clay-rich rock at the boundary between sedimentary and metamorphic rocks, makes sourcing studies more challenging.
► Sourced from one location. Presumed a local source on basis of other artifactual analyses.
► Chemical fingerprinting appears to be a useful tool in separating different fine-grained rock units in the region.

## Slide 18
In archaeological terms a local source location of the Tyros Beds represents exploration of another physical environment for the Early Helladics at Lerna.

## Slide 19: ACKNOWLEDGEMENTS
SCHRADER ARCHAEOLOGICAL ENDOWMENT FUND
HUTTON HONORS COLLEGE/PROFESSIONAL INTERNSHIP FOR H. TIMM
M. WIENCKE/ HEAD OF LERNA EXCAVATIONS PUBLICATIONS
EPHOREIA FOR ANTIQUITIES/NAUPLION, GREECE
RUTH DROPPO, Graphic Artist
DEPARTMENT OF GEOLOGICAL SCIENCES, INDIANA UNIVERSITY